## Slide 1: Mg Alloys
Clancy and Weihs Group

## Slide 2: Target: Corrosion Rate
Notes: Meet with Sreenivas and talk about what other properties might be important.

## Slide 3: Target: Corrosion Rate
LASSO
XGBoost
Notes: Meet with Sreenivas and talk about what other properties might be important.

## Slide 4: Target: Hardness
LASSO
XGBoost
Notes: Meet with Sreenivas and talk about what other properties might be important.

## Slide 5: ST Study
26th September, 2023

## Slide 6: Microstructure vs Corrosion and HV XGBoost and PCC
XGBoost
Notes: Meet with Sreenivas and talk about what other properties might be important.

## Slide 7: Microstructure vs Hardness
LASSO
XGBoost
Notes: Meet with Sreenivas and talk about what other properties might be important.

## Slide 10: Next Steps
ST– Study Data Analysis
Discover ideal processing conditions
Notes: Meet with Sreenivas and talk about what other properties might be important.

## Slide 11: Microstructure vs Corrosion and HV XGBoost and PCC
XGBoost
Corrosion
Hardness Value
Notes: Meet with Sreenivas and talk about what other properties might be important.

## Slide 12: Next Steps
ST– Study Outline
  Assisting Sreenivas in putting together the outline for the paper
  Journal options?
    Journal of Materials Chemistry B
Notes: Meet with Sreenivas and talk about what other properties might be important.

## Slide 13: ST Paper
16th October, 2023

## Slide 14: Things to do this week
Refit the grain growth kinetics curve
Fit data to
  Guo-Sha Model (Relating Precipitate to Hardness)
  Hall – Petch Relationship (Relating Grain Size to Hardness)
  Bailey-Hirsh Model (Relating Dislocation Density to Hardness)
  Goal of doing this: What microstructure properties are dominating the targets at different solution treatment times.
Wonder if we should do some kind of symbolic regression on the data?
Notes: Is there a way to model the small time scale grain growth?
Richard Catlow – NY, Alfred University
Glass transition example
Gibbs nucleation model - too simple.
Look at phase transition barriers – Divya's idea!
Competition between: Volume vs. Surface energy
Look for possible potentials?
Phase field model – for qualitative hypothesis, transition between 2 types of growths.
Lenard Jones
MEAM potentials - https://www.sciencedirect.com/science/article/pii/S0364591614000789?via%3Dihub
Ask Sreenivas - Consistency in the samples and who made them. (Prof. Clancy)

## Slide 15: Grain Growth
Notes: Is there a way to model the small time scale grain growth?
Richard Catlow – NY, Alfred University
Glass transition example
Gibbs nucleation model - too simple.
Look at phase transition barriers – Divya's idea!
Competition between: Volume vs. Surface energy
Look for possible potentials?
Phase field model – for qualitative hypothesis, transition between 2 types of growths.
Lenard Jones
MEAM potentials - https://www.sciencedirect.com/science/article/pii/S0364591614000789?via%3Dihub
Ask Sreenivas - Consistency in the samples and who made them. (Prof. Clancy)

## Slide 16: Updated Texture and Precipitates Data

## Slide 17: Corrosion Rate
XGBoost

## Slide 18: Hardness Value
XGBoost

## Slide 19: Training Scores: Hardness
Training Scores: Corrosion

## Slide 20: Updated Data from November 2023

## Slide 21: Corrosion Rate
Hardness

## Slide 22
Hypothesis Testing for Hardness
Training Score: 0.996
Training Score: 0.997

## Slide 23
Hypothesis Testing for Hardness
0. 'Grain_size_mean’, 1. 'Disloc_den’,
2. 'Mg’, 3. 'Ca2Mg6Zn3’, 4. 'Mg2Ca’, 5. 'Mn’,
6. '10-10’, 7. '0002’, 8. '11-20’, 9. '10-10/0002’,
10. '11-20/0002'
Training Score: 0.988

## Slide 24
Hypothesis Testing for Corrosion
Training Score: 0.996
Training Score: 0.996

## Slide 25: Updated Data from November 2023

## Slide 26: Hardness Value
XGBoost

## Slide 27
Hypothesis Testing for Hardness
Training Score: 0.997
Training Score: 0.996

## Slide 28
Hypothesis Testing for Hardness
0. 'Grain_size_mean’, 1. 'Disloc_den’,
2. 'Mg’, 3. 'Ca2Mg6Zn3’, 4. 'Mg2Ca’, 5. 'Mn’,
6. '10-10’, 7. '0002’, 8. '11-20’, 9. '10-10/0002’, 10. '11-20/0002'
Training Score: 0.988
Notes: Ternary Phase and Mg difference in electrochemical potential –
Binary Phase and Mg electrochemical potential –
Mn and Mg electrochemical potential –
Ternary - 396.05
Binary - 126.42
Mn - 205.66

## Slide 29: Corrosion Rate
XGBoost

## Slide 30
Hypothesis Testing for Corrosion
Training Score: 0.996
Training Score: 0.996

## Slide 31: What to put in the paper
Correlation analysis between the target variables and the input features

## Slide 32: LASSO
Corrosion Rate
Hardness
Notes: Variables are highly correlated
Limit of these methods – Talk about which of the two methods works better. LASSO picks out texture which does not make physical sense.

## Slide 33: Literature Review
Data augmentation – 2022
NN – 2022
Random Forest – 2022, 2023
Clustering (t-SNE) – 2023
Sequential Feature Selection – 2023

## Slide 34: Sreenivas Slides

## Slide 35
Current Version
From SEM Image Analysis
From XRD Integrated Area Analysis
Notes: What’s the uncertainty here?

## Slide 36
Current Version

## Slide 37
Phase Diagram

## Slide 38
Previous Version

## Slide 39
First Version

## Slide 40
Updates Feb

## Slide 41
Feature Selection using physics-based features
Grain Boundary Strengthening
Precipitate Strengthening
Dislocation Strengthening
Notes: critical resolved shear stress

## Slide 42
Feature Selection using physics-based features
Grain Boundary Strengthening
Precipitate Strengthening
Dislocation Strengthening
Updated input features:
  Grain boundary as d-1/2
  Precipitates as Vol Frac * volta-potential difference between the intermetallic and Mg matrix
  Dislocation density as rho1/2
Notes: critical resolved shear stress

## Slide 43
Feature Selection using physics-based features
LASSO
Notes: critical resolved shear stress

## Slide 44
Feature Selection for Corrosion using physics-based features
LASSO
Notes: critical resolved shear stress

## Slide 45
Analysis Discussion
Notes: critical resolved shear stress

## Slide 46
Analysis Discussion
Notes: critical resolved shear stress

## Slide 47
Analysis Discussion
Notes: critical resolved shear stress

## Slide 48
Results for paper

## Slide 49
Feature Selection using physics-based features
Grain Boundary Strengthening
Precipitate Strengthening
Dislocation Strengthening
Notes: critical resolved shear stress

## Slide 50
Feature Selection using physics-based features
Grain Boundary Strengthening
Precipitate Strengthening
Dislocation Strengthening
Updated input features:
  Grain boundary as d-1/2
  Precipitates as Vol Frac * volta-potential difference between the intermetallic and Mg matrix
  Dislocation density as rho1/2
Notes: critical resolved shear stress

## Slide 51
Feature Selection for Hardness using physics-based features
Previous

## Slide 53
Fit for Ralston-Birbilis Model
A = 2.8217812
B = 3.22930937
R2 = 0.466

## Slide 54
Fit for Bahmani Model with only precipitates
A = 0.71593123
B = 0.1195259
R2 = 0.872

## Slide 55
Fit for complete Bahmani Model